## Slide 1: Particle Properties: Methods & Specs
Hugh Stitt & Vincenzino Vivacqua
April 2021

## Slide 2: Particle Properties – Specification ad Definition
Tradition (unfortunately still often so)
    Specs set by supplier (not us!)
  PSD – as (typically) d10, d50, d90
    Sometime d95 or d98 used
    Normally laser diffraction only
      Poor data at < 0.5 micron (fines)
  Bulk density – poured or tapped
      Rarely both or a Hausner ratio
  Composition (impurities), morphology
  Porosity – commonly (BJH) pore volume,
    Sometime (BET) surface area etc
  Suspension rheology – single rpm Brookfield
  Safety: MIE, OELs, Inhalable etc
Internal specs may be more precise
  Shape, flowability etc rarely discussed
Improvements – in progress/implementation
  Particle Size & Shape
    Concatenating laser diffraction and dynamic light scattering data – capture the fines
      Plus data driven models that infer the fines
    Representing PSD as a series of (log-Gaussian) populations (non-linear regression)
    Particle shape (mainly aspect ratio)
  Flowability
    BD is easy to measure – but we know Hausner is a poor predictor of flow
      Angle of repose not much better
    Shear cell (or sim) flow function data
  Suspension rheology
    “6 point” characterisation on Broookfield
    Full shear rate (or stress) sweep
      Future - bounds on parameters in rheology model
Tradition, progress and vision

## Slide 3: Improving Particulate System Characterisation
Technical
  For the most part the experimental methods/equipment are already known
    Requires standardisation of use
    Requires justification for local investment
  The main challenge is in getting better data interpretation
    Concatenation of LD and DLS data in a standardised way
    Improved and standardised methods for model parameter estimation
      Non linear regression & advances stats methods
      Providing “tool-boxes” : PSD peak deconvolution and rheology model fitting
Cultural
  “We’ve done it this way for years”
  Better understand critical attributes of powder for processing and product performance
      What is the ideal PSD for ……?
    Required for better definition of feed, intermediate and product attributes
  How to include these in purchase specs for incoming goods?
    Suppliers will resist additional specs
      Even at a price
    We don’t often assess incoming goods
      Rely simply on the suppliers’ CQA data
        Which may not include what’s important
Technical & Cultural
We are working hard to be better at this – methods development and “persuasion”